## Slide 1: Vanadium Oxide on Anatase (101)

## Slide 2
4NO + 4NH3 + O2 → 4N2 + 6H2O

## Slide 3: SCR-catalyst
Active phase, submonolayer-V2O5
YANG, Hua Gui, et al. Anatase TiO 2 single crystals with a large percentage of reactive facets. Nature, 2008, 453.7195: 638. Ek, Martin, et al. "Visualizing atomic-scale redox dynamics in vanadium oxide-based catalysts." Nature communications 8.1 (2017): 305.
Substrate, Anatase-TiO2
(001)
(101)

## Slide 4: Clean anatase Tio2 (101)

## Slide 5: STM of V2O5 –clusters (as-deposited)
V2O5 clusters on a-TiO2
– evaporated from metal in O2
V2O5 clusters on a-TiO2
– evaporated from powder

## Slide 6: As deposited
Imaged at room temperature
Corresponding to
coverage ~ 0.5ML
XPS – of reactive deposition

## Slide 7: Structural models

## Slide 8: Adding water
Scanning with increasing water pressure
Maximum pressure:

## Slide 9: Re-exposing
Maximum pressure:

## Slide 10: 3 features are present during the experiment
Across the rows
Before water exposure
Cherry
During water exposure
Nose
After water exposure

## Slide 11
L. Arnarson, Lauritsen, J. V., & Moses, P. G. (2015). Coexistence of Square Pyramidal Structures of Oxo Vanadium (+ 5) and (+ 4) Species Over Low-Coverage VO X/TiO2 (101) and (001) Anatase Catalysts. The Journal of Physical Chemistry C, 119(41), 23445-23452.
Most stable

## Slide 13: Another re-exposure
Across the rows
Before water exposure
Cherry
During water exposure
Nose
After water exposure

## Slide 14: Reaction
+

## Slide 15
Moving feature could be a surface hydroxyl
Reversible
20s per frame
Present under high water pressure
Formed after water pressure and stable under UHV

## Slide 16: Calculations suggestions
  Energy of VOx adsorbates
  What happens when water
  is introduced
    Possibly to include different
    chemical potentials
  Reversible interactions at ~mbar

## Slide 17: Planned experiments
- Higher coverages and slight annealing maybe during water exposure
- measure the amount of different species as function of H2O pressure.
- Low temp. water exposure
- Ammonia interaction
- eventually NO interaction

## Slide 18: Vanadia dimers has been found to split under hydration
Most Stable
Calatayud, M., Mguig, B., & Minot, C. (2005). A DFT study on the hydrated V2O5-TiO 2-anatase catalyst: stability of monomeric species. Theoretical Chemistry Accounts, 114(1-3), 29-37.
DFT calculations on (001), not (101)

## Slide 19: V2O5 cluster on TiO2 surface Structure
Global minimum : V2O5_TiO2(101)
Top view
Side view

## Slide 20: V2O5 cluster on TiO2 surface Structure
Local minima 1: V2O5_TiO2(101)

## Slide 21: V2O5 cluster on TiO2 surface Structure
Local minima 2: V2O5_TiO2(101)

## Slide 22: VO2 on TiO2 (101) Surface
Global minimum : VO2_TiO2(101)
Top view
Side view
Side view