## Slide 1: Vanadium figures

## Slide 5: model suggestions
= V
2 X VO3H
V2O5
V2O5

## Slide 6: Methodology
21 super cell top view
31 super cell top view
41 super cell top view
61 super cell top view
21 super cell side view

## Slide 7: VO2 Clusters with Ov (1by2 Super cell)
I1:

## Slide 8: VO2 + H2O Clusters with Ov (1by2 Super cell)
I1:
I2:
I3:
I4:
I1:

## Slide 9: VO2 + 2H2O Clusters with Ov (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 10: V2O4 Clusters with Ov (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 11: V2O4 Clusters with Ov (1by3 Super cell)
I6:
I7:

## Slide 12: V2O4 + H2O Clusters with Ov (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 13: V2O4 + H2O Clusters with Ov (1by3 Super cell)
I7:
I8:
I9:
I10:

## Slide 14: V2O4 + 2H2O Clusters with Ov (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 15: V2O4 + 2H2O Clusters with Ov (1by3 Super cell)
I6:
I7:
I8:
I9:
I10:

## Slide 16: V2O5 Clusters with Ov (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 17: V2O5 Clusters with Ov (1by4 Super cell)
I6:
I7:
I8:
I9:
I10:
I11:

## Slide 18
I1:
I2:
I4:
I5:
I6:
I7:
I8:
I9:
I10:
I11:
I12:
I13:
I14:
I15:
I16:
I17:
I18:
V2O5 Clusters with Ov (1by4 cell)

## Slide 19
I19:
I20:
I21:
I22:
I23:
I24:
I25:
I26:
I27:
I28:
I29:
I30:
V2O5 Clusters with Ov (1by4 cell)

## Slide 20: V2O5 Clusters with Ov (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:
I7:
I8:
I10:
I11:
I12:
I13:
I14:
I15:
I16:
I17:

## Slide 21: V2O5 Clusters with Ov (1by4 Super cell)
I18:
I19:
I20:
I21:
I22:
I23:
I24:
I25:
I26:
I27:
I28:
I29:
I30:
I31:
I32:
I33:

## Slide 22: V2O5 Clusters with Ov (1by4 Super cell)
I34:
I35:
I36:
I37:
I38:
I39:
I40:

## Slide 23
V2O5 Clusters with Ov (1by4 cell) for paper

## Slide 24
V2O5 1H2O and V2O5 2H2O Clusters with Ov (1by4 cell) for paper

## Slide 25: Method Vs Energy Order
Method (fcut=0.023 eV/Ang) | I1/ (Ov) | I2/(Ov) | I3/(Ov) | I4/(Ov)
GPAW (PW(500 eV),PBE,dzp,(2,2,1)) | 0.00 | -0.476 | -0.103 | -0.411
GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0)) | 0.000 | 0.006 | 0.106 | 0.124
GPAW (PW(500 eV),PBE,dzp,(4,4,1), U(4.0)) | 0.000 | 0.006 | 0.106 | 0.123
CP2K (GPW(400 Ry),PBE,dzvp) | 0.000 | -1.154 | -0.745 | -0.951
CP2K (GPW(400 Ry),PBE,dispersion (dftd3),dzvp) | 0.000 | -1.017 | -0.584 | -0.719
Method (fcut=0.023 eV/Ang) |  |  |  | 
GPAW (PW(500 eV),PBE,dzp,(2,2,1)) | 0.00 | -0.476 | -0.103 | -0.411
GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0)) | 0.000 | 0.006 | 0.106 | 0.124
GPAW (PW(500 eV),PBE,dzp,(4,4,1), U(4.0)) | 0.000 | 0.006 | 0.106 | 0.123
CP2K (GPW(400 Ry),PBE,dzvp) | 0.000 | -1.154 | -0.745 | -0.951
CP2K (GPW(400 Ry),PBE,dispersion (dftd3),dzvp) | 0.000 | -1.017 | -0.584 | -0.719
I1
I2
I3
I4

## Slide 26: Method Vs Energy Order
M1 = CP2K (GPW(400 Ry),PBE,dzvp)
M2 = GPAW (PW(500 eV),PBE,dzp,(2,2,1))
M1 :
M1:
M1 :
M1 :
M1 :
M1 :
M1 :
M3 = GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0))
M3 :
M2:
M2:
M2:
M2:
M2:
M2:
M2:
M3:
M3:
M3 :
M3:
M3 :
M3 :

## Slide 27
All the structures optimized with 1

## Slide 28
P298 K = 51 %
P298 K = 49 %
Calculations done in 2 only for two structures during exposure.

## Slide 29: Figures for Paper

## Slide 30: Method Vs Energy Order
M3 :
M3 :
M3 :
M3 :
M3 :
M2 = GPAW (PW(500 eV),PBE,dzp,(2,2,1))
M3 = GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0))
M2 :
M2 :
M2 :
M2 :
M2 :

## Slide 31: Method Vs Energy Order
M2 :
M2 :
M2 :
M2 :
M2 :
M3 :
M3 :
M3 :
M3 :
M3:
M2 = GPAW (PW(500 eV),PBE,dzp,(2,2,1))
M3 = GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0))
M2 :

## Slide 32: Super cells Used for Optimization
14 Super cell
2 Super cell

## Slide 33: V2O5 Ov (14 Super cell)
GPAW (PW(500 eV),PBE,dzp,(2,2,1))

## Slide 34: V2O5 + H2O with Ov (14 Super cell)
V2O5 + H2O with Ov (2 Super cell)
V2O5 + 2 H2O with Ov (14 Super cell)
V2O5 + 2 H2O with Ov (2 Super cell)
For 2 Super cell
force converged up to
0.055 eV/Ang during
optimization

## Slide 35: Binding Energy of H2O on V2O5/TiO2 (2 super cell)

## Slide 36: Binding Energy of H2O on V2O5/TiO2 (6 super cell)
Oxygen Vacancy created in 2nd layer of 2nd row
from left to right

## Slide 37: Binding Energy of H2O on V2O5/TiO2 (6 super cell with Ov)
Oxygen Vacancy created in 2nd
layer of 6th row from left to right
Oxygen Vacancy created in 2nd
layer of 2nd row from left to right

## Slide 38: Binding Energy of H2O on V2O5/TiO2 (6 super cell)
2 Oxygen Vacancies created in 2nd layer

## Slide 39
Before
During
After

## Slide 40: GPAW and CP2K
I1:
I2:
I3:
I1:
I2:
I3:
GPAW
Mode = PW
E_cut = 500 eV for plane wave
XC = PBE
U_corrct (Hubbard term) = 4.0 eV
F_cut = 0.025 eV/Ang
CP2K
Mode = GPW (gaussian and plane wave method)
E_cut = 400 Ry for plane wave
XC = PBE
Dispersion correction = DFTD3 (PBE functional)
F_cut = 0.023 eV/Ang

## Slide 41: V2O5 Clusters with Ov (1by4 Super cell)
I1:
I2:
I1:
I2:

## Slide 42: VO2 + H2O Clusters (1by2 Super cell)
I1:
I2:
I3:
I4:

## Slide 43: VO2 + 2H2O Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 44: V2O4 Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 45: V2O4 Clusters (1by3 Super cell)
I6:
I7:

## Slide 46: V2O4 + H2O Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 47: V2O4 + 2H2O Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 48: V2O4 + 2H2O Clusters (1by3 Super cell)
I6:
I7:
I8:
I9:
I10:

## Slide 49: V2O5 Clusters (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 50: V2O5 Clusters (1by4 Super cell)
I6:
I7:
I8:
I9:
I10:
I11:

## Slide 51: V2O5 Clusters (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 52: V2O5 Clusters (1by4 Super cell)
I9:
I10:
I11:
I8:
I7:

## Slide 53: V2O5 Clusters (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 54: V2O5 Clusters (1by4 Super cell)
I7:
I8:
I9:

## Slide 55: V2O6 Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 56: V2O6 Clusters (1by3 Super cell)
I7:
I8:
I9:
I10:

## Slide 57
Before H2O exposer
During H2O exposer
After H2O exposer
Global minimum
Global minimum
I2:
This becomes GM if we have
more than 2 H2O

## Slide 58
Ueff (eV) | Stoichiometric surface (eV) Ueff for only V | Reduced surface (eV) Ueff for both V & Ti | Reduced surface (eV) Ueff for only Ti | Stoichiometric surface (eV) Ueff for only Ti
4.0 | 0.128 | 0.078 | 0.103 | 0.254
3.0 | 0.136 | 0.075 |  | 
2.0 | 0.142 | 0.075 |  | 
Ueff (eV) |  |  |  | 
4.0 | 0.128 | 0.078 | 0.103 | 0.254
3.0 | 0.136 | 0.075 |  | 
2.0 | 0.142 | 0.075 |  | 
I1
I2

## Slide 59
Ueff (eV) | Stoichiometric surface (eV) Ueff for only V | Reduced surface (eV) Ueff for both V & Ti
4.0 | 0.116 | 0.095
3.0 | 0.107 | 0.056
2.0 | 0.101 | 0.890
Ueff (eV) |  | 
4.0 | 0.116 | 0.095
3.0 | 0.107 | 0.056
2.0 | 0.101 | 0.890
I1
I2

## Slide 60: Adsorption Energies By addition of H2O Molecule
Eads = Etot. (n H2O + V2O5) / a-TiO2(101)) - n Etot(H2O) - Etot((VO)x + a-TiO2(101))
 | Eads (1 H2O) (eV) | Eads (2 H2O) (eV) | Eads (3 H2O) (eV) | Eads (5 H2O) (eV)
E1Ads | -0.871 | 1.546 |  | 
E2Ads | -1.264 |  |  | 
E3Ads | -1.013 |  |  | 
E4Ads | -0.912 | -1.945 | -2.929 | -3.943
E5Ads | -1.982 | -2.875 | -3.694 | -4.838
H2O
H2O
H2O
H2O
E1Ads
E2Ads
E3Ads

## Slide 61
H2O
H2O
H2O
H2O
H2O
2 H2O
2 H2O
H2O
E4Ads
E5Ads

## Slide 62: Observations
1) Effect of O-vacancy:
There is gain in energy due to O-vacancy in the subcell surface. The gain in energy is around in the range of 0.05 eV to 0.200 eV depends upon the structure. De to this there is change in the order of low-lying isomers which are in the range of meV.
I4:
I2:
O-vacancy

## Slide 63: Observations
2) Dissociation capability of H2O due to size of Cluster:
In case of VO2 cluster, it requires 0.131 eV/1 H2O and 0.053 eV/2 H2O energy to dissociate the H2O. And In case of V2O4 and V2O5, dissociated H2O strcture is the GM.
I1:
I2:
I1:
I3:

## Slide 64: Observations
3) Surface Effect on H2O dissociation:
We did not observed the surface hydroxyls within 0.2 eV energy range from GM. Mostly Vanadium oxide clusters are responsible for H2O dissociation.
I1:
I2:
I1:
I4:

## Slide 65: Adsorption Energy order

## Slide 67: Binding Energy of H2O for V2O5+H2O (Ov+csr)
I12:E
I10:E
I9:E
I11:E
I13:E
I14:E

## Slide 68: Binding Energy of H2O for V2O5+2 H2O (Ov+csr)
I1:E
I2:E
I4:E
I6:E
I7:E
I3:E
I5:E
I1:E
I1:E
I3:E

## Slide 69: Binding Energy of H2O for V2O5+2 H2O (Ov+csr)
I12:E
I13:E
I11:E
I10:E
I9:E
I8:E

## Slide 70
I3:E
I7:E
I2:E
I1:E
I5:E
I9:E
I3:E
I4:E
I7:E
I1:E
I2:E
I5:E
I7:E
I8:E

## Slide 71
I1:E
I2:E
I3:E
I4:E
I5:E
I6:E
I8:E
I7:E
I5:E
I1:E
I5:E
I3:E
I4:E
I2:
I3:
I4:
I1:

## Slide 72: Density of States

## Slide 73: Density of States

## Slide 75: Observations
4) Dissociation of V2O5 clusters and Non-dissociation of V2O4 clusters:
In case of V2O5 clusters during H2O exposure, the cluster get dissociated in two paces (Ex: VO3H) and in case of V2O4 during H2O exposure also the clusters get remains intact due to keeping of +4 or +5 state of Vanadium oxidation state.
5) Restructuring of V2O5 cluster during H2O exposure:
The re-structuring of V2O5 cluster during water exposure is due to dissociation of H2O makes the V2O5 cluster in to two VO3H clusters and these two VO3H clusters can have different arrangements.

## Slide 76: Suggestions for a structure
2xV
6XO
4XH

## Slide 77: Suggestions for a structure
2xV
6XO
2XH

## Slide 78: Suggestions for a structure
2xV
6XO
2XH

## Slide 79
2xV
5XO
2XH
Placement of H is very uncertaint

## Slide 80
2xV
5XO

## Slide 81
H2O
1 X H2O

## Slide 82
H2O
1 X H2O

## Slide 83
H2O
1 X H2O
2 X H

## Slide 84: model suggestions
= V
2 X VO3H + 2X H_bridge
2 X VO2
2 different configurations
V2O5H2

## Slide 86
2xH2O
H2O