## Slide 1: Vanadium Oxide on Anatase (101)

## Slide 2: Clean anatase Tio2 (101)

## Slide 3: STM of V2O5 –clusters (as-deposited)
V2O5 clusters on a-TiO2
– evaporated from metal in O2
V2O5 clusters on a-TiO2
– evaporated from powder

## Slide 4: Structural models

## Slide 5: Adding water
Scanning with increasing water pressure
Maximum pressure:

## Slide 6: Re-exposing
Maximum pressure:

## Slide 7: 3 features are present during the experiment
Across the rows
Before water exposure
Cherry
During water exposure
Nose
After water exposure

## Slide 8: Another re-exposure
Across the rows
Before water exposure
Cherry
During water exposure
Nose
After water exposure

## Slide 9: Planned experiments
- Higher coverages and slight annealing maybe during water exposure
- measure the amount of different species as function of H2O pressure.
- Low temp. water exposure
- Ammonia interaction
- eventually NO interaction

## Slide 10: Anatase TiO2 (101) surface and O vacancy Anatase TiO2 (101) surface
DFT Method for Optimization:
Mode: PW
Basis = dzp
Ecut = 500 eV
Kpts = 21
Super cell : 1
DFT+U Method for Optimization of
Oxygen Vacancy TiO2:
Mode: PW
Ueff = 3.5 eV
Basis = dzp
Ecut = 500 eV
Kpts = 21

## Slide 11: VO2 Cluster
VO2
I1:

## Slide 12: Hydroxylation of VO2 Clusters
I1:
I2:
I3:
I4:
I5:

## Slide 13: Hydroxylation of VO2 Clusters
I1:
I2:
I3:
I4:
I5:

## Slide 14: Hydroxylation of VO2 Clusters
I6:
I7:
I8:
I9:

## Slide 15: V2O4 Clusters
I1:
I3:
I2:
I4:
I5:
I6:
I7:

## Slide 16: Hydroxylation of V2O4 Clusters
I1:
I2:
I5:
I6:
I3:
I4:

## Slide 17: Hydroxylation of V2O4 Clusters
I8:
I9:
I10:
I11:
I7:

## Slide 18: Hydroxylation of V2O4 Clusters
I1:
I2:
I3:
I4:

## Slide 19: Hydroxylation of V2O4 Clusters
I5:
I6:
I7:

## Slide 20: V2O5 Clusters on TiO2 (1 supercell)
I5:
I4:
I3:
I1:
I2:
I6:

## Slide 21: Hydroxylation of V2O5 Clusters
I2:
I3:
I5:
I1:
I4:

## Slide 22: Hydroxylation of V2O5 Clusters
I8:
I7:
I6:
I9:

## Slide 23: Hydroxylation of V2O5 Clusters
I10:
I11:
I14:
I12:
I13:

## Slide 24: Hydroxylation of V2O5 Clusters
I15:
I16:
I17:
I18:
I19:

## Slide 25: Hydroxylation of V2O5 Clusters
I20:
I21:
I24:
I22:
I23:

## Slide 26: Hydroxylation of V2O5 Clusters
I25:
I26:
I29:
I27:
I28:

## Slide 27: Hydroxylation of V2O5 Clusters
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 28: Hydroxylation of V2O5 Clusters
I7:
I8:
I9:
I10:
I11:
I12:

## Slide 29: Hydroxylation of V2O5 Clusters
I13:
I14:
I15:
I16:
I17:
I18:

## Slide 30: Hydroxylation of V2O5 Clusters
I19:
I20:
I21:
I22:
I23:
I24:

## Slide 31: Hydroxylation of V2O5 Clusters
I25:
I26:
I27:
I28:

## Slide 32: V2O5 Clusters on TiO2 (1 supercell)
I1:
I2:
I4:
I6:
I5:
I3:

## Slide 33: V2O5 Clusters on TiO2 (1 supercell)
I7:
I8:
I10:
I11:
I9:

## Slide 34: V2O5 Clusters on TiO2 (1 supercell)
I12:
I13:
I15:
I14:

## Slide 35: V2O5 Clusters on TiO2 (1 supercell) Complete slab relax
I1:
I2:
I5:
I6:
I4:
I3:

## Slide 36: (V2O5 + H2O) Clusters on TiO2 (1 supercell)
I1:
I2:
I3:
I4:
I5:

## Slide 37: (V2O5 + H2O) Clusters on TiO2 (1 supercell)
I7:
I8:
I9:
I10:
I6:

## Slide 38: (V2O5 + H2O) Clusters on TiO2 (1 supercell)
I12:
I13:
I14:
I15:
I11:

## Slide 39: (V2O5 + H2O) Clusters on TiO2 (1 supercell)
I17:
I18:
I19:
I16:

## Slide 40: (V2O5 + H2O) Clusters on TiO2 (1 supercell) Complete Slab Relax
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 41: (V2O5 + H2O) Clusters on TiO2 (1 supercell) Complete Slab Relax
I7:

## Slide 42: (V2O5 + 2 H2O) Clusters on TiO2 (1 supercell)
I1:
I2:
I4:
I5:
I6:
I3:

## Slide 43: (V2O5 + 2 H2O) Clusters on TiO2 (1 supercell)
I8:
I9:
I10:
I11:
I12:
I7:

## Slide 44: (V2O5 + 2 H2O) Clusters on TiO2 (1 supercell)
I13:
I14:
I15:
I16:
I16:

## Slide 45: (V2O5 + 2 H2O) Clusters on TiO2 (1 supercell) Complete Slab Relax
I1:
I2:
I3:
I5:
I4:
I6:

## Slide 46: (V2O5 + 2 H2O) Clusters on TiO2 (1 supercell) Complete Slab Relax
I7:
I8:
I7:
I8:

## Slide 47: V2O4 Clusters with Oxygen Vacancy
I1:
I2:
I3:
I4:
I5:

## Slide 48: Hydroxylation of V2O4 Clusters with Oxygen Vacancy
I1:
I2:
I3:
I5:
I4:

## Slide 49: Hydroxylation of V2O4 Clusters with Oxygen Vacancy
I6:
I7:
I8:
I10:
I9:

## Slide 50: Hydroxylation of V2O4 Clusters with Oxygen Vacancy
I1:
I3:
I4:
I5:
I2:

## Slide 51: Hydroxylation of V2O4 Clusters with Oxygen Vacancy
I6:
I7:

## Slide 52: V2O5 Clusters with Oxygen Vacancy
I4:
I3:
I1:
I2:

## Slide 53: V2O5 Clusters with Oxygen Vacancy
I6:
I7:
I5:

## Slide 54: Hydroxylation of V2O5 Clusters with Oxygen Vacancy
I1:
I2:
I3:
I4:

## Slide 55: Hydroxylation of V2O5 Clusters with Oxygen Vacancy
I5:
I6:
I7:
I8:

## Slide 56: Hydroxylation of V2O5 Clusters with Oxygen Vacancy
I9:
I10:
I11:
I12:

## Slide 57: Hydroxylation of V2O5 Clusters with Oxygen Vacancy
I13:
I14:
I15:

## Slide 58: Hydroxylation of V2O5 Clusters with Oxygen Vacancy
I1:
I2:
I3:
I4:
I5:

## Slide 59: Hydroxylation of V2O5 Clusters with Oxygen Vacancy
I6:
I7:
I8:
I9:
I10:

## Slide 60: Hydroxylation of V2O5 Clusters with Oxygen Vacancy
I11:
I12:
I13:
I14:

## Slide 61: Effect of U (on site coulomb interactions) for V2O5 clusters on TiO2 (101)
Ueff | 
0.0 | 0.296
3.0 | 0.259
4.0 | 0.226
5.0 | 0.197
3.0 (Ov) | 0.124
4.0 (Ov) | 0.131
5.0 (Ov) | 0.109
Ueff | 
0.0 | 0.296
3.0 | 0.259
4.0 | 0.226
5.0 | 0.197
3.0 (Ov) | 0.124
4.0 (Ov) | 0.131
5.0 (Ov) | 0.109
I1
I2

## Slide 62: Effect of U (on site coulomb interactions) for V2O5 + H2O clusters on TiO2 (101)
Ueff | 
0.0 | 0.092
3.0 | 0.057
4.0 | 0.030
5.0 | -0.009
3.0 (Ov) | -0.042
4.0 (Ov) | -0.104
5.0 (Ov) | -0.163
Ueff | 
0.0 | 0.092
3.0 | 0.057
4.0 | 0.030
5.0 | -0.009
3.0 (Ov) | -0.042
4.0 (Ov) | -0.104
5.0 (Ov) | -0.163
I1
I2

## Slide 63: Effect of U (on site coulomb interactions) for V2O5 + 2H2O clusters on TiO2 (101)
Ueff |  | 
0.0 | 0.002 | 0.146
3.0 | 0.113 | 0.228
4.0 | 0.144 | 0.254
5.0 | 0.181 | 0.268
3.0 (Ov) | 0.143 | 0.096
4.0 (Ov) | 0.171 | 0.123
5.0 (Ov) | 0.202 | 0.149
Ueff |  | 
0.0 | 0.002 | 0.146
3.0 | 0.113 | 0.228
4.0 | 0.144 | 0.254
5.0 | 0.181 | 0.268
3.0 (Ov) | 0.143 | 0.096
4.0 (Ov) | 0.171 | 0.123
5.0 (Ov) | 0.202 | 0.149
I1
I2
I3

## Slide 64
Before H2O exposer
During H2O exposer
After H2O exposer
Global minimum
Global minimum
I2:

## Slide 65: Energy difference between H2Odiss and H2Oundis
Cluster type | No. Of H2O | (eV)
VO2 | 1 | 0.27
VO2 (O vacancy in TiO2 surface) | 1 | 0.21
VO2 | 2 | 0.20
V2O5 | 1 | - 0.02
V2O5 | 2 | - 0.14
Cluster type | No. Of H2O | 
VO2 | 1 | 0.27
VO2 (O vacancy in TiO2 surface) | 1 | 0.21
VO2 | 2 | 0.20
V2O5 | 1 | - 0.02
V2O5 | 2 | - 0.14

## Slide 66: Experiment and Theory
Across the rows
Before water exposure
Cherry
During water exposure
Nose
After water exposure
I1:
I1:
I4:

## Slide 67: Experiment and Theory

## Slide 68: Experiment and Theory
I1:

## Slide 69
I46:
I52:
Cherry
During water exposure

## Slide 70
Nose
After water exposure
I8:
I25:
I37:

## Slide 71
I1:
I52:
I37:

## Slide 73: Binding Energy of Water Molecule
I1:
I3:
Ebind = Etot. (n H2O + V2O5) / a-TiO2(101)) - n Etot(H2O) - Etot((VO)x + a-TiO2(101))

## Slide 74: Binding Energy of Water Molecule
I2:
I6:
I8:
I37:
I44:

## Slide 75
I1:
I2:
I3:
I4:
I5:
I6:
I7:

## Slide 76
I1:
I2:
I3:
I4:
I10:

## Slide 77
E
E
E
E
E
E
E
E
E
E
E
E

## Slide 78: Oxidation of Vanadium cluster on TiO2 (101)
1) Higher Oxidation state of V(+5) is most catalytically active state.
2) Possible oxidation states for V (+2,+4,+5)
3) With increasing oxygen pressure V changes oxidation states to +2 to +5 (in progress of oxidation)
Synthesis of Vanadium oxide clusters :
1) Oxidation of vanadia clusters
VO2 (+4)or V2O5)
2) Deposition of vanadium oxide vapour clusters

## Slide 79: Energy Profile for V2O5 Lowest Structures
What is the free energy barrier for chagning the symmetry of the stucture
Which of them is the most probable stcucture at room temperature

## Slide 80
L. Arnarson, Lauritsen, J. V., & Moses, P. G. (2015). Coexistence of Square Pyramidal Structures of Oxo Vanadium (+ 5) and (+ 4) Species Over Low-Coverage VO X/TiO2 (101) and (001) Anatase Catalysts. The Journal of Physical Chemistry C, 119(41), 23445-23452.
Most stable

## Slide 81: Calculations suggestions
  Energy of VOx adsorbates
  What happens when water
  is introduced
    Possibly to include different
    chemical potentials
  Reversible interactions at ~mbar

## Slide 82
PRL, 21, 206003 (2018)