## Slide 1: Water induced Restructuring of Vanadia clusters supported on a-TiO2 (101) hydration dynamics
K. C. Adamsen et. Al.

## Slide 2: Figure 1, overview
B
A ) STM image (20 X 20 nm) of the a-TiO2 (101) after evaporation of Vanadium in 1E-6 mbar O2 , individual clusters are assigned to V2O5 clusters. B ) XP-spectra of the O1s- and V2p – region after evaporation of V in 1E-6 mbar O2 of 15% monolayer coverage. The inset highlights the V2p 3/2 region showing a 2 peak fit corresponding to the 4+ and 5+ states of vanadia. Measured with photon energy of 650 eV. C) STM image (15 X 15 nm) of V2O5/a-TiO2 (101) after water exposure
D) STM image (15 X 15 nm) of V2O5/a-TiO2 (101) during water exposure (6torr)
A
D
C

## Slide 3: Figure 3, statistics
Second exposure
First exposure
A

## Slide 4: Figure 2, individual structures
+ H2O
- H2O
+ H2O
A
B
C
V2O5/a-TiO2
Dimer
2 X VO3H + H2O /a-TiO2
Hydrated
2 X VO3H /a-TiO2
Dehydrated

## Slide 5: Figures for Paper

## Slide 6: DFT figure
+ 2 x H2O
- H2O
+ H2O

## Slide 8: Additional informations and alternative figures

## Slide 9: Figure 1, overview
B
A ) STM (50 X 50 nm) image of the clean a-TiO2 (101). B) STM image (50 X 50 nm) of the a-TiO2 (101) after evaporation of Vanadium in 1E-6 mbar O2 , individual clusters are assigned to V2O5 clusters. C ) XP-spectra of the O1s- and V2p – region after evaporation of V in 1E-6 mbar O2 of 15% monolayer coverage. The inset highlights the V2p 3/2 region showing a 2 peak fit corresponding to the 4+ and 5+ states of vanadia.
A
C
New clean surface image

## Slide 10: DFT model , not ready yet

## Slide 11: Figure 2
B
A
C
A ) STM image of V205 particle before water dose. The as-deposited feature extents across two Obr–rows (vertical orange guide-lines) and is centered on-top of one Obr– site (between two horizontal guide-lines) B) STM image of V205 particle during water dose. This feature has a two major features on-top of fully coordinated Ti-6f sites, together with two minor features on the adjacent row. This feature has a mirror plan going through its horizontal center. C) STM image of V205 particle after water dose. This feature has a lesser bright feature broad feature (extending 2 sites) on top of the fully coordinated Ti-6f site, in one row and bright feature on-top of the Ti-5f site.
Maybe line-scans could be a nice addition