## Slide 1: Vanadium figures

## Slide 5: model suggestions
= V
2 X VO3H
V2O5
V2O5

## Slide 6: VO2 Clusters with Ov (1by2 Super cell)
I1:

## Slide 7: VO2 + H2O Clusters with Ov (1by2 Super cell)
I1:
I2:
I3:
I4:

## Slide 8: VO2 + 2H2O Clusters with Ov (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 9: V2O4 Clusters with Ov (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 10: V2O4 Clusters with Ov (1by3 Super cell)
I6:
I7:

## Slide 11: V2O4 + H2O Clusters with Ov (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 12: V2O4 + H2O Clusters with Ov (1by3 Super cell)
I7:
I8:
I9:
I10:

## Slide 13: V2O4 + 2H2O Clusters with Ov (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 14: V2O4 + 2H2O Clusters with Ov (1by3 Super cell)
I6:
I7:
I8:
I9:
I10:

## Slide 15: V2O5 Clusters with Ov (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 16: V2O5 Clusters with Ov (1by4 Super cell)
I6:
I7:
I8:
I9:
I10:
I11:

## Slide 17
I1:
I2:
I4:
I5:
I6:
I7:
I8:
I9:
I10:
I11:
I12:
I13:
I14:
I15:
I16:
I17:
I18:
V2O5 Clusters with Ov (1by4 cell)

## Slide 18
I19:
I20:
I21:
I22:
I23:
I24:
I25:
I26:
I27:
I28:
I29:
I30:
V2O5 Clusters with Ov (1by4 cell)

## Slide 19: V2O5 Clusters with Ov (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:
I7:
I8:
I10:
I11:
I12:
I13:
I14:
I15:
I16:
I17:

## Slide 20: V2O5 Clusters with Ov (1by4 Super cell)
I18:
I19:
I20:
I21:
I22:
I23:
I24:
I25:
I26:
I27:
I28:
I29:
I30:
I31:
I32:
I33:

## Slide 21: V2O5 Clusters with Ov (1by4 Super cell)
I34:
I35:
I36:
I37:
I38:
I39:
I40:

## Slide 22: Method Vs Energy Order
Method (fcut=0.023 eV/Ang) | I1/ (Ov) | I2/(Ov) | I3/(Ov) | I4/(Ov)
GPAW (PW(500 eV),PBE,dzp,(2,2,1)) | 0.00 | -0.476 | -0.103 | -0.411
GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0)) | 0.000 | 0.006 | 0.106 | 0.124
GPAW (PW(500 eV),PBE,dzp,(4,4,1), U(4.0)) | 0.000 | 0.006 | 0.106 | 0.123
CP2K (GPW(400 Ry),PBE,dzvp) | 0.000 | -1.154 | -0.745 | -0.951
CP2K (GPW(400 Ry),PBE,dispersion (dftd3),dzvp) | 0.000 | -1.017 | -0.584 | -0.719
Method (fcut=0.023 eV/Ang) |  |  |  | 
GPAW (PW(500 eV),PBE,dzp,(2,2,1)) | 0.00 | -0.476 | -0.103 | -0.411
GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0)) | 0.000 | 0.006 | 0.106 | 0.124
GPAW (PW(500 eV),PBE,dzp,(4,4,1), U(4.0)) | 0.000 | 0.006 | 0.106 | 0.123
CP2K (GPW(400 Ry),PBE,dzvp) | 0.000 | -1.154 | -0.745 | -0.951
CP2K (GPW(400 Ry),PBE,dispersion (dftd3),dzvp) | 0.000 | -1.017 | -0.584 | -0.719
I1
I2
I3
I4

## Slide 23: Method Vs Energy Order
M1 = CP2K (GPW(400 Ry),PBE,dzvp)
M2 = GPAW (PW(500 eV),PBE,dzp,(2,2,1))
M1 :
M1:
M1 :
M1 :
M1 :
M1 :
M1 :
M3 = GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0))
M3 :
M2:
M2:
M2:
M2:
M2:
M2:
M2:
M3:
M3:
M3 :
M3:
M3 :
M3 :

## Slide 24
All the structures optimized with 1

## Slide 25
P298 K = 51 %
P298 K = 49 %
Calculations done in 2 only for two structures during exposure.

## Slide 26: Figures for Paper

## Slide 27: Method Vs Energy Order
M3 :
M3 :
M3 :
M3 :
M3 :
M2 = GPAW (PW(500 eV),PBE,dzp,(2,2,1))
M3 = GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0))
M2 :
M2 :
M2 :
M2 :
M2 :

## Slide 28: Method Vs Energy Order
M2 :
M2 :
M2 :
M2 :
M2 :
M3 :
M3 :
M3 :
M3 :
M3:
M2 = GPAW (PW(500 eV),PBE,dzp,(2,2,1))
M3 = GPAW (PW(500 eV),PBE,dzp,(2,2,1), U(4.0))
M2 :

## Slide 29: Super cells Used for Optimization
14 Super cell
2 Super cell

## Slide 30: V2O5 Ov (14 Super cell)
GPAW (PW(500 eV),PBE,dzp,(2,2,1))

## Slide 31: V2O5 + H2O with Ov (14 Super cell)
V2O5 + H2O with Ov (2 Super cell)
V2O5 + 2 H2O with Ov (14 Super cell)
V2O5 + 2 H2O with Ov (2 Super cell)
For 2 Super cell
force converged up to
0.055 eV/Ang during
optimization

## Slide 32: Binding Energy of H2O on V2O5/TiO2 (2 super cell)
EBE of H2O on TiO2 (2 super cell) = 0.625 eV (still fmax not converged)

## Slide 33: GPAW and CP2K
I1:
I2:
I3:
I1:
I2:
I3:
GPAW
Mode = PW
E_cut = 500 eV for plane wave
XC = PBE
U_corrct (Hubbard term) = 4.0 eV
F_cut = 0.025 eV/Ang
CP2K
Mode = GPW (gaussian and plane wave method)
E_cut = 400 Ry for plane wave
XC = PBE
Dispersion correction = DFTD3 (PBE functional)
F_cut = 0.023 eV/Ang

## Slide 34: V2O5 Clusters with Ov (1by4 Super cell)
I1:
I2:
I1:
I2:

## Slide 35: VO2 + H2O Clusters (1by2 Super cell)
I1:
I2:
I3:
I4:

## Slide 36: VO2 + 2H2O Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 37: V2O4 Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 38: V2O4 Clusters (1by3 Super cell)
I6:
I7:

## Slide 39: V2O4 + H2O Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 40: V2O4 + 2H2O Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 41: V2O4 + 2H2O Clusters (1by3 Super cell)
I6:
I7:
I8:
I9:
I10:

## Slide 42: V2O5 Clusters (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:

## Slide 43: V2O5 Clusters (1by4 Super cell)
I6:
I7:
I8:
I9:
I10:
I11:

## Slide 44: V2O5 Clusters (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 45: V2O5 Clusters (1by4 Super cell)
I9:
I10:
I11:
I8:
I7:

## Slide 46: V2O5 Clusters (1by4 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 47: V2O5 Clusters (1by4 Super cell)
I7:
I8:
I9:

## Slide 48: V2O6 Clusters (1by3 Super cell)
I1:
I2:
I3:
I4:
I5:
I6:

## Slide 49: V2O6 Clusters (1by3 Super cell)
I7:
I8:
I9:
I10:

## Slide 50
Before H2O exposer
During H2O exposer
After H2O exposer
Global minimum
Global minimum
I2:
This becomes GM if we have
more than 2 H2O

## Slide 51
Ueff (eV) | Stoichiometric surface (eV) Ueff for only V | Reduced surface (eV) Ueff for both V & Ti | Reduced surface (eV) Ueff for only Ti | Stoichiometric surface (eV) Ueff for only Ti
4.0 | 0.128 | 0.078 | 0.103 | 0.254
3.0 | 0.136 | 0.075 |  | 
2.0 | 0.142 | 0.075 |  | 
Ueff (eV) |  |  |  | 
4.0 | 0.128 | 0.078 | 0.103 | 0.254
3.0 | 0.136 | 0.075 |  | 
2.0 | 0.142 | 0.075 |  | 
I1
I2

## Slide 52
Ueff (eV) | Stoichiometric surface (eV) Ueff for only V | Reduced surface (eV) Ueff for both V & Ti
4.0 | 0.116 | 0.095
3.0 | 0.107 | 0.056
2.0 | 0.101 | 0.890
Ueff (eV) |  | 
4.0 | 0.116 | 0.095
3.0 | 0.107 | 0.056
2.0 | 0.101 | 0.890
I1
I2

## Slide 53: Adsorption Energies By addition of H2O Molecule
Eads = Etot. (n H2O + V2O5) / a-TiO2(101)) - n Etot(H2O) - Etot((VO)x + a-TiO2(101))
 | Eads (1 H2O) (eV) | Eads (2 H2O) (eV) | Eads (3 H2O) (eV) | Eads (5 H2O) (eV)
E1Ads | -0.871 | 1.546 |  | 
E2Ads | -1.264 |  |  | 
E3Ads | -1.013 |  |  | 
E4Ads | -0.912 | -1.945 | -2.929 | -3.943
E5Ads | -1.982 | -2.875 | -3.694 | -4.838
H2O
H2O
H2O
H2O
E1Ads
E2Ads
E3Ads

## Slide 54
H2O
H2O
H2O
H2O
H2O
2 H2O
2 H2O
H2O
E4Ads
E5Ads

## Slide 55: Observations
1) Effect of O-vacancy:
There is gain in energy due to O-vacancy in the subcell surface. The gain in energy is around in the range of 0.05 eV to 0.200 eV depends upon the structure. De to this there is change in the order of low-lying isomers which are in the range of meV.
I4:
I2:
O-vacancy

## Slide 56: Observations
2) Dissociation capability of H2O due to size of Cluster:
In case of VO2 cluster, it requires 0.131 eV/1 H2O and 0.053 eV/2 H2O energy to dissociate the H2O. And In case of V2O4 and V2O5, dissociated H2O strcture is the GM.
I1:
I2:
I1:
I3:

## Slide 57: Observations
3) Surface Effect on H2O dissociation:
We did not observed the surface hydroxyls within 0.2 eV energy range from GM. Mostly Vanadium oxide clusters are responsible for H2O dissociation.
I1:
I2:
I1:
I4:

## Slide 58: Adsorption Energy order

## Slide 60: Binding Energy of H2O for V2O5+H2O (Ov+csr)
I12:E
I10:E
I9:E
I11:E
I13:E
I14:E

## Slide 61: Binding Energy of H2O for V2O5+2 H2O (Ov+csr)
I1:E
I2:E
I4:E
I6:E
I7:E
I3:E
I5:E
I1:E
I1:E
I3:E

## Slide 62: Binding Energy of H2O for V2O5+2 H2O (Ov+csr)
I12:E
I13:E
I11:E
I10:E
I9:E
I8:E

## Slide 63
I3:E
I7:E
I2:E
I1:E
I5:E
I9:E
I3:E
I4:E
I7:E
I1:E
I2:E
I5:E
I7:E
I8:E

## Slide 64
I1:E
I2:E
I3:E
I4:E
I5:E
I6:E
I8:E
I7:E
I5:E
I1:E
I5:E
I3:E
I4:E
I2:
I3:
I4:
I1:

## Slide 65: Density of States

## Slide 66: Density of States

## Slide 68: Observations
4) Dissociation of V2O5 clusters and Non-dissociation of V2O4 clusters:
In case of V2O5 clusters during H2O exposure, the cluster get dissociated in two paces (Ex: VO3H) and in case of V2O4 during H2O exposure also the clusters get remains intact due to keeping of +4 or +5 state of Vanadium oxidation state.
5) Restructuring of V2O5 cluster during H2O exposure:
The re-structuring of V2O5 cluster during water exposure is due to dissociation of H2O makes the V2O5 cluster in to two VO3H clusters and these two VO3H clusters can have different arrangements.

## Slide 69: Suggestions for a structure
2xV
6XO
4XH

## Slide 70: Suggestions for a structure
2xV
6XO
2XH

## Slide 71: Suggestions for a structure
2xV
6XO
2XH

## Slide 72
2xV
5XO
2XH
Placement of H is very uncertaint

## Slide 73
2xV
5XO

## Slide 74
H2O
1 X H2O

## Slide 75
H2O
1 X H2O

## Slide 76
H2O
1 X H2O
2 X H

## Slide 77: model suggestions
= V
2 X VO3H + 2X H_bridge
2 X VO2
2 different configurations
V2O5H2

## Slide 79
2xH2O
H2O