## Slide 1: Stability and Oxidation of Supported (-Al2O3 (0001)) Pt-clusters

## Slide 2: Aim of the Project
Effect of size on structure of Pt clusters:
Pt7, Pt8, Pt10, Pt13 (In order to see the structural trends and also to explain the structure-property relationship)
Oxidation of Pt clusters:
Effect of O2 on structure of Pt clusters with increasing number of O2
Effect of water on Pt clusters:
It can change the adsorption properties of molecules on surfaces of heterogeneous catalysis reactions

## Slide 3: Gas phase Pt clusters
I1:
I2:
I1:
I2:
I1:
I2:
I1:
I2:
Pt7 cluster
Pt8 cluster
Pt10 cluster
Pt13 cluster

## Slide 4: -Al2O3 Surface Preparation (0001)
Bulk Unit cell : a=4.806
Bulk Unit cell : a=4.784
Energy fitness
Strain filter
ase.surface()
Vaccume gap : 12
Super cell : 331
Total No. Of Atoms:270
Only 135 atoms are
Allowed for GOFEE
Time taken for SP calc.
Is average 10 minutes
in GOFEE

## Slide 5: On-the fly Fitting of KRR Model(GOFEE)
Generate Initial Population
Train the Model
Generate new child structures with mutation operations
Relax with Model
Select best fitness structure
Up date the population
Calculate SP DFT
SP DFT setup:
Mode: LCAO
Basis set: dzp
Kpts=111

## Slide 6: Lowest Energy Structures of Pt7 clusters
I2:
I3:
I4:
I1:
I5:
I6:
I7:
I8:
I9:
I10:
I11:
I12:
1) Alexandrova et al., J. Phys. Chem. Lett. 2018, 9, 1696−1702.

## Slide 7: Pt7 Success rate
Pt7 O12 Success rate
Pt7 O10 Success rate

## Slide 8: Structural Evolution of Pt7 with increasing O2
I4:
I1:
I2:
I3:
I2:
Pt7O2
Pt7O4
Pt7O6
Pt7O8
Pt7O10
Pt7O12

## Slide 9: Energy Level Diagram for Pt7Ox(x=0) + CO
I1:
I2:
I5:
I3:
I4:
I6:
I7:
I1:
I2:
I3:
I4:
I5:
I6:
I7:

## Slide 10: Energy Level Diagram for Pt7Ox(x=0,4) + CO
I1:
I2:
I6:
I4:
I5:
I7:
I8:
I3:
I1:
I2:
I6:
I4:
I5:
I7:
I8:
I3:
I1:
I2:
I3:
I4:
I5:
I6:
I7:

## Slide 11: Energy Level Diagram for Pt7Ox(x=0,10) + CO
I1:
I2:
I4:
I3:
I1:
I2:
I3:
I4:
I5:
I1:
I2:
I3:
I4:
I5:
I6:
I7:

## Slide 12
Pt7O4
Pt7O10
Pt7
CO
CO
CO2
CO
CO2
?

## Slide 13
UHV chamber
ALD-Pt7/Al2O3(0001)
CO2
1 % (CO + O2) + He
Partial pressure =8 Torr
CO + O2 Pt –O-O-C-O-Pt CO2

## Slide 14: Stability of Pt7 Oxides
Pt7O2
Pt7O4
Pt7O6
Pt7O12
Pt7O14
Pt7O8
Pt7O10
Pt7
Pt7O2
Pt7O4
Pt7O6
Pt7O8
Pt7O10
Pt7O12
Pt7O14
Ef = 0.00 eV
Ef = -4.23 eV
Ef = -8.23 eV
Ef = -11.70 eV
Ef = -13.67 eV
Ef = -15.74 eV
Ef = -17.27 eV
Ef = -18.64 eV
Ef = -17.32 eV
Pt7O18
Pt7O18
-4.23 eV
-4.00 eV
-3.47 eV
-1.97 eV
-2.07 eV
-1.53 eV
-1.37 eV
1.32 eV

## Slide 15: Adsorption Energies of CO

## Slide 16: GM structures for Pt-Oxide/Al2O3Clusters and Ads./Chem. of CO
Adsorption of CO on Pt7Oy
CO + Pt7Oy Pt7OyCO
Pt7
Pt7O2
Pt7O4
Pt7O6
Pt7O8
Pt7O10
Pt7O12
Pt7O14
Pt7O16

## Slide 17: Success Rate of Pt-Oxides with CO Chemisorption
Pt7
70% (14/20 restarts)
N_itr=500
Pt7O2
35% (7/20 restarts)
N_itr=1000
Pt7O4
50% (10/20 restarts)
N_itr=1000
Pt7O6
41% (7/17 restarts)
N_itr=2000
Pt7O8
10% (2/20 restarts)
N_itr=1500
Pt7O10
50% (10/20 restarts)
N_itr=1500
Pt7O12
40% (8/20 restarts)
N_itr=1000
Pt7O14
10% (2/20 restarts)
N_itr=1000
Pt7O16
30% (3/10 restarts)
N_itr=1000
Pt7CO (GM)
35% (7/20 restarts)
N_itr=850
Pt7O2CO(GM)
20% (2/10 restarts)
N_itr=1100
Pt7O4CO(GM)
5% (1/20 restarts)
N_itr=850
Pt7O4CO (LM1)
20% (4/20 restarts)
N_itr=850
Pt7O4CO (LM2)
20% (4/20 restarts)
N_itr=850
Pt7O2CO(LM1)
30% (3/10 restarts)
N_itr=1100
Pt7CO (lM1)
15% (3/20 restarts)
N_itr=850
Pt7O2CO(GM)
20% (2/10 restarts)
N_itr=1100

## Slide 18
Pt7O6CO(GM)
20% (2/10 restarts)
N_itr=900
Pt7O6CO
20% (2/10 restarts)
N_itr=900
Pt7O8CO(GM)
13% (2/15 restarts)
N_itr=900
Pt7O8CO(lM1)
13% (2/15 restarts)
N_itr=900
Pt7O10CO(GM)
26% (4/15 restarts)
N_itr=1000
Pt7O12CO(lm)
20% (2/10 restarts)
N_itr=900
Pt7O14CO(GM)
20% (3/15 restarts)
N_itr=800
Pt7O16CO(GM)
10% (1/10 restarts)
N_itr=750
Pt7O12CO(GM)
20% (2/10 restarts)
N_itr=900

## Slide 19: Stability of Pt7-Oxides with CO

## Slide 20
Pt7

## Slide 21
Pt7O1

## Slide 22: Fig 2
Pt7O2
Pt7O2CO

## Slide 23
Pt7O3

## Slide 24: Fig 3
Pt7O4
Pt7O4CO

## Slide 25
Pt7O5

## Slide 26: Fig 4
Pt7O6
Pt7O6CO

## Slide 27
Pt7O7

## Slide 28: Fig 5
Pt7O8

## Slide 29: Extra Stability of Pt7O2CO
Pt7+O
Pt7O + O
Pt7O2 + CO
Pt7O2 + CO
Pt7O2 + CO
CO + Pt7O2
Pt7 + CO
- CO2

## Slide 30: Fig 6
Pt7O10
Pt7O10CO

## Slide 31: Fig 7
Pt7O12
Pt7O12CO

## Slide 32: Fig 8
Pt7O14
Pt7O14CO

## Slide 33: Fig 9
Pt7O16
Pt7O16CO

## Slide 35
Pt7CO
Pt7O2CO
Pt7O4CO
Pt7O6 CO
Pt7O8CO
Pt7O10CO
Pt7O12CO
Pt7O14CO
Pt7O16CO

## Slide 37: Lowest Energy Structures of Pt7 + x O2 Clusters
I1:
I2:
I3:
I4:
I5:
I6:
I7:
I8:
I1:
I2:
I3:
I4:
I5:
I6:
I7:
I8:
I1:
I2:
I3:
I4:
I5:
I6:
I7:
I8:
Pt7O2
Pt7O4
Pt7O6

## Slide 38: Lowest Energy Structures of Pt7 + x O2 Clusters
Pt7O8
Pt7O10

## Slide 39: Lowest Energy Structures of Pt7 + x O2 Clusters
I1:
I2:
I3:
I4:
I5:
I6:
I7:
I8:
I1:
I2:
I3:
I1:
I2:
I3:
Pt7O12
Pt7O14
Pt7O18

## Slide 40: Lowest Energy Structures of Pt10 clusters
I1:
I2:
I3:
I4:
I5:
I6:
I7:
I8:
I9:
I10:
I11:
I12:

## Slide 41: Pt10 Success rate
Pt10 O18 Success rate
Pt10 O12 Success rate

## Slide 42: Structural Evolution of Pt10 with increasing O2
I1:
I4:
I5:
I9:
Pt10O2
Pt10O4
Pt10O6
Pt10O12
Pt10O18
Pt10O20

## Slide 43: Stability of Pt10 Oxides with increasing O2
Pt10O20
Pt10O18
Pt10O12
Pt10O6
Pt10O4
Pt10O2

## Slide 44: Lowest Energy Structures of Pt10 + x O2 Clusters
I1:
I2:
I3:
I4:
I1:
I2:
I3:
I4:
I1:
I2:
I3:
I4:
I1:
I2:
I3:
I4:
I1:
I2:
I3:
I4:
Pt10O2
Pt10O4
Pt10O6
Pt10O12
Pt10O20

## Slide 45: Lowest Energy Structures of Pt13 clusters
I1:
I2:
I3:
I4:
I5:
I6:
I7:
I8:
I9:
I10:
I11:
I12:

## Slide 46: Pt13 Success rate
Pt13 O18 Success rate

## Slide 47: Structural Evolution of Pt13 with increasing O2
I2:
I1:
I2:
I3:
Pt13O2
Pt13O4
Pt13O6
Pt13O12
Pt13O18

## Slide 48: Stability of Pt13 Oxides with increasing O2
Pt13O2
Pt13O4
Pt13O6
Pt13O12
Pt13O18

## Slide 49: Lowest Energy Structures of Pt13 + x O2 Clusters
I1:
I2:
I3:
I4:
I1:
I2:
I3:
I4:
I1:
I2:
I3:
I4:
I1:
I2:
I3:
I1:
Pt13O6
Pt13O2
Pt13O4
Pt13O12
Pt13O18

## Slide 50: Lowest Energy Structures of Pt8 clusters
2) Alexandrova et al., ACS Catal. 2017, 7, 3322−3335.
I1:
I2:
I3:
I4:
I5:
I6:
I8:
I9:
I10:
I11:
I12:
I7:

## Slide 51: Pt7 Success rate
Pt8 Success rate

## Slide 52: Structural Evolution from Pt7 to Pt13
I1:
I2:
I1:
I1:
I1:
I2:
I2:
I2:

## Slide 53: Oxidation of Pt7, Pt10 and Pt13 Clusters

## Slide 54: Future Work
Pt13O26 compositions need to do GO.
We need to see how the catalytic property changes by transformation from cluster to single layer Pt-oxide structures and also size effect.
It will be interesting to know the catalytic properties with respect to ensemble average of different low-lying isomers.